Arabo Bag filters collector
Arabo Filters not only builds full dust collector systems; we also manufacture the essential components—filter bags and cages—from scratch. Whether you need new bags for a custom system or replacements for an existing setup, Arabo delivers tailor‑made solutions precisely matched to your equipment and dust profile
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AI-generated content may be incorrect.]Arabo Filters designs and manufactures high-performance filter bags that form the core of every dust collection system. Whether for new installations or replacing bags in existing units, our solutions are custom-sized and locally produced, ensuring seamless fit, fast delivery, and unmatched quality. We offer a wide range of media—including Polyester, Polypropylene, PPS (Ryton®), Nomex® (Aramid), Acrylic, and Antistatic-treated fabrics—each engineered for optimal air permeability, tensile strength, and chemical resistance. Every bag is tailored to withstand your operating conditions, from 90°C to 240°C, and resist abrasion, moisture, acids, alkalis, and hydrolysis. With full vertical integration, Arabo delivers not just the collector—but the heart of it, built to last.
Markets/applications section
Food & Beverage, Fertilizers, Cement, metalurgical, mining.

Related Products:
Filter Cages – Filter Bags – Cartridge Dust Collector
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Generic Name

Common Trade 

Name

Continuous 

Temperature

Peak 

Temperature 

Abrasion Hydrolysis

Acidic 

resistance

Alkalic 

resistance

Polyester Dacron® 135 

℃

150 

℃

4 1 2 1

Polypropylene Polypropylene 90 

℃

120 

℃

4 4 4 4

Acrylic Orlon® 125 

℃

135 

℃

3 3 3 3

Polyphenylene 

Sulphide (PPS)

Ryton® 190 

℃

200 

℃

3 4 4 4

Aromatic Polyamide Nomex® 204 

℃

220 

℃

4 2 2 3

General characteristics Chemical Resistance

FILTER BAGS MATERIAL


